## Slide 1: Monolithic 3D DRAM Technology
Deepak C. Sekar, Brian Cronquist, Israel Beinglass, Paul Lim, Zvi Or-Bach
15th June 2011
MonolithIC 3D Inc. Patents Pending

## Slide 2: Outline
Status of the DRAM industry today
Monolithic 3D DRAM
Implications and risks of the technology
Summary

## Slide 3: Outline
Status of the DRAM industry today
Monolithic 3D DRAM
Implications of the technology
Summary

## Slide 4: DRAM makers fall in the “endangered species” category
Why? What are the challenges? We’ll see in the next few slides
Samsung Hyundai
Micron Siemens
NEC Hitachi
Mitsubishi Toshiba
Fujitsu LG Semicon
TI-Acer Vanguard
Powerchip ProMOS
Winbond Oki
IBM TI
Motorola Matsushita
Seiko Epson Nippon Steel
UMC Mosel Vitelic
1996
24 key DRAM players
Samsung
Hynix
Micron
Elpida
Nanya
Inotera
Powerchip
ProMOS
Winbond
2010
9 key DRAM players

## Slide 5: Reason 1: Profitability
DRAM has not been a profitable business in the near past
Balance sheets of most companies’ DRAM businesses similar to above 
Financials of a top-tier DRAM vendor (Elpida) vs. fiscal year

## Slide 6: Reason 2: Large fab cost for scaling-down
Scaling-down  lower cost per bit  but huge litho and fab investment
Hard for unprofitable companies to fund scaled-down fabs
Source: Morgan Stanley
Today,
Litho Tool Cost = $42M
Etch, CVD, Implant, RTA tools each cost <$5M

## Slide 7: Reason 3: Scaling-down the stacked capacitor challenging
Requires >150:1 aspect ratios and exotic new high-k dielectrics!
 | 45nm | 32nm | 22nm | 15nm | 10nm
Dielectric constant | 40 | 50 | 60 | 65 | 70
Aspect ratio | 47:1 | 56:1 | 99:1 | 147:1 | 193:1
EOT | 0.8nm | 0.6nm | 0.5nm | 0.3nm | 0.2nm
Source: ITRS 2010
Al2O3 (90nm)  HfO2 (80nm)
 ZrO2 (60nm)  ?
Capacitance
Keep ~25fF
Memory Cell Transistor
Keep low leakage current

## Slide 8: Reason 4: The cell transistor needs major updates on scaling-down
A major new transistor every generation or two!
100nm Planar  80nm RCAT  60nm S-RCAT  35nm Finfet (?)  20nm Vertical (?)

## Slide 9: To recap, Things don’t look good for DRAM vendors because
Low profitability
Cost of scaled-down fabs
Scaling-down stacked capacitor
Cell transistor scaling-down
Related
Common theme  Scaling-down
Is there an alternative way to reduce DRAM bit cost other than scaling-down?
Focus of this presentation

## Slide 10: Outline
Status of the DRAM industry today
Monolithic 3D DRAM
Implications of the technology
Summary

## Slide 11: Key technology direction for NAND flash: Monolithic 3D with shared litho steps for memory layers
To be viable for DRAM, we require
Single-crystal silicon at low thermal budget  Charge leakage low
Novel monolithic 3D DRAM architecture with shared litho steps
Toshiba BiCS
Poly Si
Samsung VG-NAND
Poly Si
Macronix junction-free NAND
Poly Si

## Slide 12: Single crystal Si at low thermal budget
Obtained using the ion-cut process. It’s use for SOI shown above.
Ion-cut used for high-volume manufacturing SOI wafers for 10+ years.
Activated p Si
Oxide
Oxide
H
Top layer
Bottom layer
Oxide
Hydrogen implant
of top layer
Flip top layer and
bond to bottom layer
Oxide
H
Cleave using 400oC
anneal or sideways
mechanical force. CMP.
Oxide
Activated p Si
Activated p Si
Activated p Si
Silicon
Silicon
Silicon
Top layer

## Slide 13: Double-gated floating body memory cell well-studied in Silicon (for 2D-DRAM)
0.5V, 55nm channel length
900ms retention
Bipolar mode
Hynix + Innovative Silicon
VLSI 2010
Intel
IEDM 2006
2V, 85nm channel length
10ms retention
MOSFET mode

## Slide 14: Our novel DRAM architecture
n+
n+
n+
Gate Electrode
Gate Dielectric
p
SiO2
Innovatively combines these well-studied technologies
Monolithic 3D with litho steps shared among multiple memory layers
Stacked Single crystal Si with ion-cut
Double gate floating body RAM cell (below) with charge stored in body

## Slide 15: Process Flow: Step 1 Fabricate peripheral circuits followed by silicon oxide layer
Silicon Oxide
Peripheral circuits with W wiring

## Slide 16: Process Flow: Step 2 Transfer p Si layer atop peripheral circuit layer
Silicon Oxide
p Silicon
H implant
Silicon Oxide
Peripheral circuits
Silicon Oxide
Peripheral circuits
Top layer
Bottom layer
Silicon Oxide
p Silicon
H implant
Flip top layer and bond to bottom layer

## Slide 17: Process Flow: Step 3 Cleave along H plane, then CMP
Silicon Oxide
Peripheral circuits
Silicon Oxide
p Silicon
Silicon Oxide
Peripheral circuits

## Slide 18: Process Flow: Step 4 Using a litho step, form n+ regions using implant
Silicon Oxide
Peripheral circuits
Silicon Oxide
p
n+
n+
n+
p

## Slide 19: Process Flow: Step 5 Deposit oxide layer
Silicon Oxide
Peripheral circuits
Silicon Oxide
Silicon Oxide
n+
p

## Slide 20: Process Flow: Step 6 Using methods similar to Steps 2-5, form multiple Si/SiO2 layers, RTA
Silicon Oxide
Peripheral circuits
Silicon Oxide 06
Silicon Oxide
Silicon Oxide 06
Silicon Oxide
Silicon Oxide 06
Silicon Oxide
p
n+
n+

## Slide 21: Process Flow: Step 7 Use lithography and etch to define Silicon regions
Silicon Oxide
Peripheral circuits
p Silicon
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon oxide
Symbols
n+ Silicon
This n+ Si region will act as wiring for the array… details later

## Slide 22: Process Flow: Step 8 Deposit gate dielectric, gate electrode materials, CMP, litho and etch
Silicon Oxide
Peripheral circuits
n+ Silicon
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon oxide
Symbols
Gate electrode
Gate dielectric

## Slide 23: Process Flow: Step 9 Deposit oxide, CMP. Oxide shown transparent for clarity.
Silicon Oxide
Peripheral circuits
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon oxide
Word Line (WL)
WL current path
SL current path
Source-Line (SL)
n+ Silicon
Silicon oxide
Symbols
Gate electrode
Gate dielectric
Silicon oxide

## Slide 24: Process Flow: Step 10 Make Bit Line (BL) contacts that are shared among various layers.
Silicon Oxide
Peripheral circuits
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon oxide
WL
SL
WL current path
SL current path
BL contact
n+ Silicon
Silicon oxide
Symbols
Gate electrode
Gate dielectric
Silicon oxide
BL contact

## Slide 25: Process Flow: Step 11 Construct BLs, then contacts to BLs, WLs and SLs at edges of memory array using methods in [Tanaka, et al., VLSI 2007]
Silicon Oxide
Peripheral circuits
n+ Silicon
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon oxide
Symbols
Gate electrode
Gate dielectric
Silicon oxide
WL
SL
SL current
BL contact
BL
WL current
BL current
BL

## Slide 26: Some cross-sectional views for clarity. Each floating-body cell has unique combination of BL, WL, SL

## Slide 27: A different implementation: With independent double gates
BL
BL contact
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
Silicon Oxide 06
p Silicon
Silicon oxide
n+ Silicon
Periphery
WL wiring
Gate dielectric
Gate electrode
BL
WL
SL

## Slide 28: Outline
Status of the DRAM industry today
Monolithic 3D DRAM
Implications and risks of the technology
Summary

## Slide 29: Density estimation
 | Conventional stacked capacitor DRAM | Monolithic 3D DRAM with 4 memory layers
Cell size | 6F2 | Since non self-aligned, 7.2F2
Density | x | 3.3x
Number of litho steps | 26 (with 3 stacked cap. masks) | ~26 (3 extra masks for memory layers, but no stacked cap. masks)
3.3x improvement in density vs. standard DRAM, but similar number of critical litho steps!!!
Negligible prior work in Monolithic 3D DRAM with shared litho steps, poly Si 3D doesn’t work for DRAM (unlike NAND flash) due to leakage

## Slide 30: Scalability
Multiple generations of cost per bit improvement possible
(eg) 22nm 2D 
22nm 3D 2 layers 
22nm 3D 4 layers  ...
Use same 22nm litho tools for 6+ years above. Tool value goes down 50% every 2 years  Cheap 
Avoids cost + risk of next-gen litho

## Slide 31: Reduces or avoids some difficulties with scaling-down
EUV delays and risk
(EETimes 2002)
"EUV to be in production in 2007"
(EETimes 2003)
"EUV to be leading candidate for the 32nm node in 2009"
(EETimes 2004)
"EUV to be pushed out to 2013"
(EETimes 2010)
"EUV late for 10nm node milestone in 2015"
Capacitor manufacturing
 | 45nm | 32nm | 22nm | 15nm | 10 nm
ε | 40 | 50 | 60 | 65 | 70
AR | 47 | 56 | 99 | 147 | 193
Continuous transistor updates
Planar  RCAT  S-RCAT  Finfet
 Vertical devices

## Slide 32: Risks
Floating-body RAM
Retention, reliability, smaller-size devices, etc
Cost of ion-cut
Supposed to be <$50-75 per layer since one implant, bond, cleave, CMP step. But might require optimization to reach this value.

## Slide 33: Outline
Status of the DRAM industry today
Monolithic 3D DRAM
Implications and risks of the technology
Summary

## Slide 34: Summary of Monolithic 3D DRAM Technology
3.3x density of conventional DRAM, but similar number of litho steps
Scalable (eg) 22nm 2D  22nm 3D 2 layers  22nm 3D 4 layers  ...
Cheap depreciated tools, less litho cost + risk, avoids many cap. & transistor upgrades
Risks = Floating body RAM, ion-cut cost
Monolithic 3D with shared litho steps
Single crystal Si
Floating body RAM
Under development...

## Slide 35: Backup slides

## Slide 36: A note on overlay
Implant n+ in p Si regions layer-by-layer, then form gate
 non self-aligned process
ITRS <20% overlay requirement
ASML 1950i = 3.5nm overlay for 38nm printing. <10% overlay.
So, gate length = 1.2F. Penalty of 0.2F for non-self-aligned process

## Slide 37: Bias schemes for floating body RAM
Bipolar Mode [S. Alam, et al, TED 2010]
MOS Mode [Intel, IEDM 2006]

## Slide 38: Contact processing with shared litho steps
Similar to Toshiba BiCS scheme [VLSI 2007]